## Slide 1
Jake Herba,b, Anushka Dasguptab, Craig Arnoldc
a Department of Chemistry b Department of Chemical and Biological Engineering c Princeton Institute for the Science and Technology of Materials
Challenges for magnesium-ion electrolytes?
The lack of electrolytes that simultaneously possess high Coulombic efficiency, conductivity, and voltage stability has hindered the deployment of rechargeable magnesium-ion batteries. The tenacious oxide layer on magnesium metal has limited the scope of research to halide ion-based electrolytes2,3,4, which limit the working voltage window considerably.
The Princeton Environmental Institute funded work on this project during the summer and the School of Engineering and Applied Sciences supported this work during the academic year through the Lidow Thesis Fund. The authors acknowledge Elizabeth Seibel and Kristen Baroudi of the Cava Lab at Princeton University for their assistance in the preparation and characterization of Mo6S8.
Herb J. T. ; Nist-Lund, C. A. ; Arnold, C.B. ACS Energy Lett. 2016, 1, 1227-1232.
Liao, C.; Guo, B.; Jiang, D.; Custelcean, R.; Mahurin, S. M.; Sun, X.-G.; Dai, S; J. Mater. Chem. A 2014, 2, 581−584.
Herb, J. T.; Nist-Lund, C.; Schwartz, J.; Arnold, C. B. ECS Electrochem. Lett. 2015, 4, A49−A52.
Muldoon, J.; Bucur, C. B.; Oliver, A. G.; Zajicek, J.; Allred, G. D.; Boggess, W. C. Energy Environ. Sci. 2013, 6, 482−487.
Weakly coordinating [Al(HFIP)4]−anions show reversible plating and stripping of magnesium with high coulombic efficiency. In addition, their high conductivity and anodic stability make them promising candidates for high voltage Mg-Ion batteries.
Synthesis
High Anodic Stability
Project Overview
Electrochemical Analysis of an Electrolyte for Magnesium-Ion Batteries1
Arnold Lab
Acknowledgements
References
Materials and Methods
H2O
No aqueous solutions
Constraints and Challenges
Conclusion
A Full Battery
AlCl3
Corrosion at higher cell potentials
To a cooled mixture of 1,1,1,3,3,3 Hexafluoroisopropanol (HFIP) in Dimethylether (DME) we added Trimethylaluminium.
To a mixture of HFIP in DME we added magnesium methoxide.
The precursors (1) and (2) were mixed in a 1:2 molar ratio and dissolved in DME. The initially cloudy mixture turned clear after stirring for 96 hours.
This work
A new magnesium electrolyte previously developed in the Arnold Lab by Dr. Jake Herb1 is synthesized and tested. A solution of fluoroalkoxyaluminate anions in DME solvent , it is shown to reversibly deposit magnesium metal with near unit efficiency in addition to achieving suitable oxidative stabilities (>3.5 V vs Mg/Mg2+ on glassy carbon and gold) and conductivities (>6 mS cm−1).
HFIP=
3.0V
3.5V
Control
3.5 V Potential Hold
0.25 M Mg[Al(HFIP)4)2 in DME
99.999% Al
MgClO4
Simple salt solutions do not facilitate Mg electrodeposition
Solvation of Mg2+ Cations
Even in long-term tests, the electrolyte is stable at voltages well above 3.0V on Aluminum metal.
The peak in the spectrum at 875 cm-1 is shown in literature to result from the presence of Mg2+ ions encaged by solvent molecules.